# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

## PRODUCT INFORMATION

26-7R

All Weather Colored Electrical Tape

Product Description:

26-7R is a colored PVC Electrical Insulation Tape with a Rubber based adhesive, which is flame retardant and cold weather resistant used general for insulating, protection, and color-coded of electrical wires; for wire harnessing in automotive industry.

TECHNICAL DATA

PROPERTY. Backing; Plasticized PVC. Adhesive; Rubber based. Total Thickness; 7 Mil (0.18mm). Voltage Breakdown; 8kv. Peel Adhesion; 16.4oz/in. Tensile Strength; 14.8 lbs/in. Elongation at Break; 200%. Temperature Resistance; 14ºF to +176ºF. Core listed; UL/CSA/CE. COLORS AVAILABLE. Black, Yellow, Green, Orange, Purple, White, Red, Blue, Gray & Brown.