# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

## PRODUCT INFORMATION

28-10R

Industrial Grade Cloth Duct Tape

Product Description:

28-10R is a Medium Grade polyethylene-coated cloth with a natural rubber adhesive.  This tape will conform well to irregular surface, and will not twist of curl during application.  Also, has excellent water and abrasion resistance, tape is hand-tearable (cutting tools not required) and tape tears evenly across web.

Performance & Application Information:

The 28-10R series is used as a quality waterproof packaging tape for export shipments; for splicing, vinyl repair, protecting, and bundling; for ductwork sealing and seaming; and for color coding.

TECHNICAL DATA

PROPERTY. Backing; Polyethylene-coated cloth. Adhesive; Natural Rubber Resin. Total Thickness; 10.2 mil +/-0.4 mils. Peel Adhesion; 39 oz/inch width. Tensile Strength; 18 lbs/inch. Application Temperature; -31ºF to 176ºF. COLORS AVAILABLE:. Silver (gray), Black, White, Yellow, Schoolbus Yellow, Sky Blue, Teal Blue, Dark Blue, Pink, Red, Burgundy, Purple, Racing Orange, Tan(Beige), Dark Brown, Light Green, Dark Green and Olive Drab. *Tape meets 90% of shelf life requirements of one year from date of shipment. Note the shelf life is dependent upon storage in a controlled environment – moderate temperature and humidity conditions..