CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com. PRODUCT INFORMATION

38-__F-GG Polycarbonate Film Gloss/Gloss

PRODUCT DESCRIPTION

Clear general purpose polycarbonate film that delivers superior impact and clarity. APPLICATIONS: Automotive, Labels, Membrane Switches, Nameplates, Packaging

PHYSICAL PROPERTIES:

PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Specific Gravity; 1.2; ASTM D792. Conversion Factor; 160; ft²/lb-mil. Water Absorption (Immersion @ 73ºF 24 hrs.); 0.33; %; ASTM D570. First Surface Gloss- 60º angle, black inked second surface; ≥98; Gloss unit; ASTM D2457. First Surface Roughness R3Z; ≥0.5; Microns; ISO 4288. THERMAL PROPERTIES: PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Heat Deflection Temp.; ISO 75. 1.62 Mpa; 270; ºF. 0.45 Mpa; 288; ºF. Viscat Softening Temp.; 315; ºF; ISO 306. OPTICAL PROPERTIES: PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Haze; 0.3; %; ASTM D1003. Light transmission; 91; %; ASTM D1003. Yellowness index; 1; ASTM E313.

MECHANICAL PROPERTIES: PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Tensile Strength, Yield; 8,800; Psi; ASTM D882. Tensile Strength, Break; 8,700; Psi; ASTM D882. Elongation @ Break; 120; %; ASTM D882. Tear Strength, Initiation; 1,100; Lb/in; ASTM D1004.