CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com. PRODUCT INFORMATION

38-__F-VM Polycarbonate Film Velvet/Matte

PRODUCT DESCRIPTION

Clear, translucent polycarbonate film with first surface velvet and a second surface matte.

PHYSICAL PROPERTIES:

PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Specific Gravity; ASTM D792. Conversion factor; 160; ft²/lb-mil. Water absorption (immersion @ 73ºF 24 hours); 0.33; %; ASTM D5470. First surface gloss 80º angle, black inked second surface; 3.0-4.5; Gloss unit; ASTM D2457. First surface roughness R3Z; 16-23; Microns; ISO 4288. THERMAL PROPERTIES: PROPERTY; TYPICAL VALUE; UNITS; TEST METHOD. Heat deflection temperature; ISO 75. 1.82 mpa; 270; ºF. 0.45 mpa; 288; ºF. Vicat softening temperature; 315; ºF; ISO 306.

MECHANICAL PROPERTIES:

| PROPERTY | TYPICAL VALUE | UNITS | TEST METHOD |
| --- | --- | --- | --- |
| Tensile strength, yield | 8,700 | Psi | ASTM D882 |
| Tensile strength, break | 8,600 | Psi | ASTM D882 |
| Elongation@break | 120 | $ | ASTM D882 |
| Tear strength, initiation | 1,100 | Lb/in | ASTM D1004 |

OPTICAL PROPERTIES:

| PROPERTY | TYPICAL VALUE | UNITS | TEST METHOD |
| --- | --- | --- | --- |
| Haze |  | % | ASTM D1003 |
| Light transmission | 90 | % | ASTM D1003 |
| Yellowness index | 1 |  | ASTM E313 |