CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com. PRODUCT INFORMATION

46-__F HYTREL 7246 FILM

PHYSICAL PROPERTIES:

Property; Test Method; Units; Value. Mechanical. Tensile Stress; ISO 8256; kJ/m2; 300. Strain 10%. Strain 5%. Yield Stress; ISO 527-1/2; MPa. 50mm/min; 30. Stress at Break; ISO 527-1/2; MPa; 45,8. Nominal Strain at Break; ISO 527-1/2; %. 50mm/min; >50. Strain at Break; ISO 527-1/2; %; 360. Yield Strain; ISO 527-1/2; %. 50mm/min; 25. Tensile Modulus; ISO 527-1/2; MPa. 1mm/min; 525. Tensile Creep Modulus; ISO 899; MPa. 1000h; 312. 1h; 360. Flexural Modulus; ISO 178; MPa. -40C; 2410. 23C; 570. 100C; 207. Notched Izod Impact; ASTM D 256/A; J/m. -40C; 40. 23C; 210. Notched Charpy Impact; ISO 179/1eA; kJ/m2. -30C; 5. 23C; 30. Unnotched Charpy Impact; ISO 179/1eU; kJ/m2. -30C; No break. 23C; No break.