# CS Hyde Company                              PRODUCT INFORMATION

FAX: 800-441-8063

53 Series

Mechanical Grade PTFE (Teflon®) coated fiberglass fabric

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

Product Description:

The 53 Series fabric is a Mechanical grade material that has a textured, non-stick surface.  This material is constructed of a PTFE (Teflon®) coated woven fiberglass substrate.  The 53 Series exhibits moderate release properties and high resistance to heat.  Ideal for applications that require a mechanical impression that can be transferred to a seal where surface texture is required.  This material is also FDA compliant (21 CFR177.1550).

Performance & Application Information:

These products are designed for applications requiring cost effective solutions.  This material can operate in temperatures from -100°F (-73°C) to   550°F under dynamic conditions (288°C). This product series has the benefits of dimensional stability, durability, excellent tensile strength and extremely low elongation (<1%).  Applications include: Impulse/L-Bar sealing, heat transfer presses, rubber curing presses, vacuum bagging, protective curtains, release sheets and many more.

### TYPICAL PROPERTIES

|  | 53-3 | 53-5 | 53-6 | 53-8 | 53-10 | 53-14 |
| --- | --- | --- | --- | --- | --- | --- |
| Nominal Thickness (in.) | .003 | .005 | .006 | .008 | .010 | .014 |
| Nominal Weight (lb./yd²) | .20 | .37 | .48 | .66 | .80 | 1.10 |
| Tensile Warp(lbs/in. of width) | 56 | 100 | 100 | 200 | 200 | 320 |
| Edge Tear Warp (grams) | 380 | 800 | 800 | 1400 | 1400 | 3700 |
| Edge Tear Fill (grams) | 250 | 700 | 700 | 1100 | 1100 | 3200 |
| Tensile Fill (lbs/sq.in) | 32 | 112 | 112 | 160 | 160 | 232 |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.  Teflon® is a registered trademark of DuPont.