| CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com. PRODUCT INFORMATION |
| --- |
| 54-SERIES Tear Resistant Grade PTFE (Teflon®) coated Fiberglass Fabric |  |  |  |  |  |
| PRODUCT DESCRIPTION |  |  |  |  |  |
| The 54 Series fabric is a Tear Resistant grade material that has a non-stick surface. This material is constructed of a PTFE (Teflon®) coated woven fiberglass substrate and a proprietary additive for flexibility. The 54 Series exhibits excellent release properties and high resistance to heat. Ideal for applications that require a minimal mechanical impression and excellent flexibility. This material is also FDA compliant (21 CFR177.1550). APPLICATION INFORMATION These products are designed for applications requiring cost effective solutions. This material can operate in temperatures from -100°F (-73°C) to 550°F under dynamic conditions (288°C). This product series has the benefits of dimensional stability, durability, excellent tensile strength and extremely low elongation (<1%). Applications include: Impulse/L-Bar sealing, heat transfer presses, rubber curing presses, vacuum bagging, protective curtains, release sheets and many more. |  |  |  |  |  |
| PHYSICAL PROPERTIES |  |  |  |  |  |
|  | 54-3 | 54-5 | 54-6 | 54-10 | 54-28 |
| Nominal Thickness (in.) | .003 | .005 | .006 | .010 | .028 |
| Nominal Weight (lb./yd²) | .27 | .48 | .54 | .94 | Proprietary |
| Tensile Warp(lbs/sq in) | 56 | 100 | 100 | 200 | Proprietary |
| Edge Tear Warp (grams) | 760 | 1600 | 1600 | 2800 | >6400 |
| Edge Tear Fill (grams) | 500 | 1400 | 1400 | 2200 | >6400 |
| Tensile Fill (lbs/sq.in) | 32 | 112 | 112 | 160 | Proprietary |