CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com. PRODUCT INFORMATION

60-7 SERIES Teflon® Coated Kevlar

PRODUCT DESCRIPTION

Teflon coated Kevlar® Fabrics are engineered to maintain their unique flexibility, dimensional stability, dielectric and tensile strength, and non-stick properties, while performing under the harshest environmental conditions. These fabrics are abrasion, tear, puncture, fire and chemical resistant; they also maintain their unique properties under pressure and extreme temperatures: -100° F to 575° F (-73° C to 302° C). USDA and NSF approval for direct food contact and are FDA compliant (21 CFR177.1550).

PHYSICAL PROPERTIES

| Property | Value |
| --- | --- |
| Fiber | Teflon® Coated Kevlar |
| Weight | .41 (Lbs. /Sq. Yard) |
| Thickness | .007” (Nominal) |
| Edge Tear Warp | 2800 (Grams) |
| Edge Tear Fill | 2800 (Grams) |
| Tensile-Warp | 160 (Lbs. /Sq. Yard) |
| Tensile-Fill | 160 (Lbs. / Sq. Yard) |