CS Hyde Company. 1351 N. Milwaukee Ave., Lake Villa, IL 60046 USA. 70-Silicone.

## Silicone Coated Fiberglass

PRODUCT DESCRIPTION

Silicone coated fiberglass is engineered to retain the distinctive properties but by adding a glass fabric to the matrix, we are able to obtain the added benefits of dimensional stability, excellent tensile strength and extremely low elongation (<1%). USDA approval for food processing and handling, and FDA compliant (21 CFR177.1550). In addition, our materials operate in temperatures from -400°F (-240°C) under static conditions and -100°F (-73°C) under dynamic conditions up to 500°F (260°C). TYPICAL APPLICATIONS - Shrink packaging – bundling - Baking and cooking – Manufacturing of flavorants - UV curing of wood products - Tank seals and containment barriers – Gaskets, membranes, seals and diaphragms Protective curtains and aprons

Product ID; Color; Plys; Friction Surface; Nominal Thickness; Weight (lbs/sq. yd.); Tensile Warp (lbs/sq. in.); Tensile Fill (lbs/sq. in.); Recommended Min. Pulley Dia.; Maximum Widths (in.). 70-10R; Red; 1; N; .010"; 0.62; 120; 100; 3"; 38*. 70-15R; Red; 1; N; .015"; 0.87; 250; 200; 3"; 38*. 70-18R; Red; 1; N; .018"; 1.05; 525; 375; 3"; 38*. 70-20R; Red; 1; Y; .020"; 1.15; 525; 375; 3"; 50*. 70-25R; Red; 1; N; .025"; 1.44; 525; 375; 3"; 50*. 70-42R; Red; 2; Y; .042"; 2.05; 1050; 750; 3"; 50*. 70-62R; Red; 3; Y; .060"; 3.07; 1575; 1125; 3"; 50*. 70-10W; White; 1; N; .010"; 0.62; 120; 100; 3"; 38*. 70-15W; White; 1; N; .015"; 0.87; 250; 200; 3"; 38*. 70-18W; White; 1; N; .018"; 1.05; 525; 375; 3"; 38*. 70-20W; White; 1; Y; .020"; 1.15; 525; 375; 3"; 50*. 70-25W; White; 1; N; .025"; 1.44; 525; 375; 3"; 50*. 70-42W; White; 2; Y; .042"; 2.05; 1050; 750; 3"; 50*. 70-62W; White; 3; Y; .060"; 3.07; 1575; 1125; 3"; 50*.