# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

## PRODUCT INFORMATION

Medical Grade

Solid Silicone Rubber,

50 durometer

71-MED

Product Description:

# Medical Grade silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance. This material is low volatile, peroxide free; platinum cured and does not discolor over time.  Silicone is odorless, tasteless, chemically inert and non-toxic.  It offers all FDA approved ingredients, low compression set and fungus resistance.  Medical Grade silicone is able to pass a flammability rating of UL94 HB.

Common Applications:

# Silicone rubber can be used for insulating and cushioning electronic assemblies.  It is used for burn victims to prevent bacteria, tubing for feeding and drainage, compression bars, electrosurgical hand pieces, infusion sleeves and test chambers, LCD displays, sensors for lasers and assemblies, gaskets, seals, food and cosmetic services, heat sealing and packaging and grommets.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Rubber |
| --- | --- | --- |
| Specific Gravity, G/CC | ASTM D297 | 1.15 |
| Durometer, Shore A | ASTM D2240 | 50 +/- 5 |
| Tensile Strength, psi | ASTM D412 | 1200 |
| Elongation, % | ASTM D412 | 600 |
| Tear, psi Die “B” | ASTM D624 | 150 |
| Temperature Range | ºF | -103 to +450 |

Available Industry Specifications:

USP Class 6, CFR 177.2600, ASTM D2000