# CS Hyde Company                               PRODUCT INFORMATION

FAX: 800-441-8063

Silicone Self Fusing Tape,

78-Series

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

Product Description:

# Silicone Rubber Self-Fusing Tape is a high performance, extruded wrapping tape. No adhesive is required. SSF Tape is self-adhering, self-fusing and permanent.  It fuses in minutes and cures in 24 hours at room temperature.  Faster curing and a harder finish are accomplished by applying heat after wrapping.  Temperature range is -60°C to 250°C for continuous use; -65C to +260C for intermittent use.

Common Applications:

Automatic wrapping, electrical insulation, moisture protection, high or low temperature applications, SSF is thermally conductive which allows generated heat to dissipate rapidly.  Used in Military, aerospace, industrial motor and marine applications including utility cable terminations and splices, bus bar insulation, motor coil terminal connections, and fuel line and hose repair.  SSF can even be applied UNDERWATER!   Silicone Self-Fusing Tape is the perfect alternative to adhesive electrical tape, duct tape, and heat shrink tape for many applications.  It withstands UV Rays, acids, weather, water and Ozone.

### TYPICAL PROPERTIES

| Property | Test Method | Performance |
| --- | --- | --- |
| Operating Temperature Range | Continuous | -130˚F to +500˚F |
|  | Intermittent | -145˚F to +500˚F |
| Dielectric Strength, | ASTM D-149 | 0.010” x -0.030” 400 VPM |
| Minimum |  | 0.040” 300VPM |
| Short TIME |  | 0.050” 275 VPM |
| (1/4; Electrodes) |  | 0.070” – 0.080: 200 VPM |
| Dielectric Constant, 1 KHZ |  | 2.95 |
| Dissipation Factor, 1 KHZ |  | <.0004 |
| Volume Resistivity | ASTM D257 | 1 x 10 OHM/CM |
| Cold Brittle Point, MAX | ASTM D-2137 | -65˚C |
| Water Absorption | FED, STD. 601, Method 6251 | 3% Max. by Weight |
| Tensile Strength | ASTM D-412 | 700 PSI Minimum |
| Ultimate Elongation | ASTM D-412 | 300% Minimum |
| Aging Property | ASTM D-412 |  |
| Retention (100 Hrs @ 500˚F) |  |  |
| TENSILE |  | 75% |
| ELONGATION |  | 50% |
| Tear Resistance | ASTM D-624 | 85 PSI |
| Durometer Hardness |  | 50 (+/- 5) Shore Durometer |
|  |  | (Room Cured 24 Hours) |
| Tolerances |  |  |
| THICKNESS |  | +/- .002” |
| WIDTH |  | +/-. 0625” |

CERTIFICATIONS

Tapes are manufactured under ISO9001:2008 certification. Products can also be

certified to many of the following specifications upon request.

Tape Cross Section Bonded Cross Section

• MIL-I-46852C, Type I & Type II

• A-A-59163, Type I & Type II

• MIL-I-22444C

• Boeing DMS2186 Type 1 & Type 2

• Lockheed Martin MMS J517

• Lockheed Martin 5-00857

• General Electric A50A493

• General Electric A50E112

• General Dynamics P5384

• Rohr RMS315, Type I, II, III

• FAR 25.853 & UL94 (upon request)