CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com. PRODUCT INFORMATION

D-WRAP Polyester Tape

PRODUCT DESCRIPTION

D-Wrap is a 1mil blue high temperature high tensile polyester film coated with a fully cured silicone adhesive. There is no contamination problem from the silicone adhesive because it is fully cured and does not transfer.

APPLICATION INFORMATION

D-Wrap is multi purpose high temperature tape designed for holding or masking operations in metal bond and plastic shops. Today it is in many other areas throughout the plant in chemical milling, riveting and paint shops. It is used as a mask on panels subject to caustic or acid bath etching. D-Wrap has also been recommended for use by aircraft companies on metal surfaces that have been phosphoric anodized because it releases clean without leaving a residue.

TECHNICAL DATA

PROPERTY; TEST METHOD; DATA. Backing Material; Polyester Film. Backing Thickness (in.); .001. Adhesive System; Silicone. Adhesive Thickness (in.); .003. Adhesion (oz/in.); ASTM-D 1000; 35. Min/Max. Operating Temp. (ºF); -100F to 310F. Tensile Strength (lb./in); ASTM-D 3759; 20. Elongation; ASTM-D 3759; 100%. Dielectric Strength; ASTM-D 149; 4,500 Volts. AVAILABILITY. Core I.D.; 3". Width (in.); .25-36. Roll Length; 36yds.