CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com. PRODUCT INFORMATION

K271 – K272 – K275 Thermally Conductive Silicone Coated KAPTON® Tape

PRODUCT DESCRIPTION

K275 is manufactured with a 1.0 mil thick thermally conductive KAPTON® film. The film is coated on both sides with 2.0 mils of thermally conductive acrylic pressure sensitive adhesive. K275 is provided in roll form with a release liner on both sides for ease of application. The product was designed to bond electrical components to heat sinks. K275 contains no halides or silicones. K272 is a thermally conductive high dielectric insulator manufactured with a 1.5 mil thick thermally conductive KAPTON® film. The film is coated on both sides with 2.0 mils of thermally conductive silicone rubber. K272 was designed for use in high performance electronics and power supplies where low thermal resistance and high dielectric strength are required. The material can be supplied with a thermally conductive acrylic adhesive on one side for applications requiring self-adhering performance. K271 is manufactured with a 1.0 mil thick thermally conductive KAPTON® film. The film is coated on one side with 1.5 mils of thermally conductive acrylic pressure sensitive adhesive, and on the other side with 2.0 mils of thermally conductive silicone rubber. K271 is provided in roll form with a release liner for ease of application. This product was designed for use in thermally conductive gaskets for high performance electronics where low thermal resistance and high dielectric strength are required.

PHYSICAL PROPERTIES:

Test Method; K275; K272; K271. Color; White; Green/White. Thickness (mils); ASTM D1000; 5.0; 6.0; 4.5. Thermal Conductivity (W/mK); ASTM E1530; 0.40; 0.90; 0.60. Thermal Impedance @ 10psi (ºC in²/W); ASTM E1530@10 psi; 0.49; 0.30; 0.30. Dielectric Strength (volts); ASTM D149; 6,500; 7,000; 7,000. Adhesion to Steel (oz./in.); ASTM D1000; 30; 30.0. Operating Temperature Range (ºF); -20 to 300; -20 to 300; -20 to 300. Flame Rating (oz./in.); UL94; Pending VTM-0.