CS Hyde Company 1351 N. Milwaukee Ave. Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com. PRODUCT INFORMATION

60-24K 100% KEVLAR STYLE W374 / 8 oz/Square Yard

PRODUCT DESCRIPTION

Kevlar® 8 oz. woven fabric. Kevlar® is 60” wide and sold by the lineal foot. Kevlar® is high heat resistant, cut resistant (CUT RESISTANCE @ 25 MM FORCE 603 GRAMS) and very strong. It is difficult to ignite, does not propagate flame and decomposes at 900ºF.

TYPICAL USES

Protective sleeves, gloves, aprons, welding blankets, heat shields/ heat barriers, hot metal sheet and glass handlers.

STYLE:	W374

FIBER:	100% KEVLAR

WEAVE: 	2 X 1 TWILL

WEIGHT:	8 OUNCES PER SQUARE YARD

WIDTH:	60 – 62”

THICKNESS:  .024 - .027”

ABRASION RESISTANCE:	150 CYCLES TO HOLD (H18 @ 1000 GMS)

CUT RESISTANCE @ 25 MM FORCE	603 GRAMS

VERTICAL FLAME PER ASTM D6413-99

AFTER FLAME	AFTERGLOW	CHAR LENGTH

(SECONDS)		(SECONDS)			(MM)

L	0			10.4			9

W	0			9.3			11