CS Hyde Company. 1351 N. Milwaukee Ave Lake Villa, IL 60046 USA 800-461-4161 / Fax: 847-395-0535 www.cshyde.com / sales@cshyde.com. 7-100S.

## Strip-N-Stick® Tape

PRODUCT DESCRIPTION

This tape is a silicone sponge with a high temperature silicone adhesive. It offers the compressibility of a medium compression closed cell sponge with a silicone pressure sensitive adhesive on one side. It is odorless, non-corrosive and non-toxic.

APPLICATION INFORMATION

Strip-N-Stick® Tape offers superior service life, excellent conformability, and flexibility. Other benefits include low compression set and high adhesion to a variety of substrates. Often chosen for high and low temperature resistance, gasketing, vibration dampening, and thermal insulation.

TECHNICAL DATA

PROPERTY; # DATA. Thickness Available (inches); 1/16”, 3/32”, 1/8”, 3/16”. Adhesive Type; Silicone. Adhesion (oz/in.); 15. Tensile Strength (lbs./in.); 65. Elongation (%); 150. Compression Deflection (comp.75% of original); 10. Compression Set % (50% compression, 22 hrs. @ 212ºF); 25. Temperature Range (ºF); -100 to +500.