CS Hyde Company. 1351 N. Milwaukee Ave., Lake Villa, IL 60046 USA 800-461-4161 / Fax: 847-395-0535 www.cshyde.com / sales@cshyde.com. 7-300AR.

## Strip-N-Stick® Tape

PRODUCT DESCRIPTION

This tape is offers the unique construction of a fiberglass reinforced medium compression closed cell silicone sponge with an aggressive acrylic adhesive. Its unique construction provides the compressibility of sponge and the dimensional stability of fiberglass reinforcement. Stretch is eliminated, which contributes to the consistent size and shape of cut parts and inhibits outward extrusion under high pressure. This also allows for close tolerance slitting. It is odorless, non-corrosive and non-toxic.

APPLICATION INFORMATION

Strip-N-Stick® Tape offers superior service life, excellent conformability, and flexibility. Other benefits include low compression set and high adhesion to a variety of substrates. Often chosen for high and low temperature resistance, gasketing, vibration dampening, and thermal insulation.

TECHNICAL DATA

PROPERTY; # DATA. Thickness Available (inches); 1/16”, 1/8”, 3/16”. Adhesive Type; Acrylic. Adhesion (oz/in.); 30. Tensile Strength (lbs./in.); 180. Elongation (%); <10. Compression Deflection (comp.75% of original); 15. Compression Set % (50% compression, 22 hrs. @ 212ºF); 25. Temperature Range (ºF); -20 to +325.