P.T.F.E. Thread Seal Tape

Specifications

Chemical Properties: Minimum of 99% Polytetrafluorethelene

Thickness: 0.0035”, +0.001 or –0.0005”

Elongation: Minimum of 50% (most of the time far exceeds this)

Width: Nominal width +0.02, -0.02

Length: Nominal length +20”, 0”

Density: 0.4

Pressure Rating: Up to 10,000 PSI

Incompatibility: Avoid using on Molten Alkali, certain Halogen products and Fluorine

at high temperatures and pressures.

Temperature: When heated over 260°C, it will thermally degrade and decompose

producing toxic fumes.

Government Standard: Meets MIL-spec T-27730A

Usage: To be used on all types of threaded fittings for passage of water potable and

non-potable, most chemicals, oxygen, gas, hydraulic and high-pressure lines.