# CS Hyde Company                            PRODUCT INFORMATION

    - FAX: 800-441-8063

1351 North Milwaukee Avenue

17- 407/409 Series

Foil – Glass Laminate w/ Silicone Adhesive

# Lake Villa, IL  60046

Product Description:

# The 17-407 and 17-409 Series are a combination of foil and glass fabric laminates with a high temperature SILICONE adhesive.  The aluminum foil provides superior conductive and reflective characteristics in high temperature applications.  The silicone adhesive demonstrates excellent adhesion at elevated temperatures yet it will remove cleanly.

Performance & Application Information:

These two foil tapes are used for masking purposes in plasma flame spray.  These tapes work best where heat reflection and conduction are needed.  They can also be used in applications that require heat shielding, such as harness wraps.

# TYPICAL PROPERTIES

|  | Test Method | 17-407 | 17-409 |
| --- | --- | --- | --- |
| Foil Thickness (in.) | ASTM-D 374 | .001 | .002 |
| Glass Fabric Thickness (in.) |  | .0025 | .0025 |
| Adhesive Thickness (in.) | ASTM-D 374 | .0035 | .004 |
| Adhesion (oz./in.) | ASTM-D 1000 | 55 | 55 |
| Tensile Strength | ASTM-D 1000 | 100 | 100 |
| Maximum Operating Temp. |  | 500ºF | 500ºF |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.