# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

52 Series

PTFE (Teflon®) coated fiberglass fabric

Product Description:

The 52 Series fabric is a multi-purpose material that has a slick, non-stick surface.  This material is constructed of a PTFE (Teflon®) coated woven fiberglass substrate.  The 52 Series exhibits exceptional release properties and high resistance to heat, chemicals and moisture.  PTFE fluorocarbon resin is one of the most chemically inert materials available. It is also highly resistant to wear, tear, cut through and breakage, even under conditions of extreme temperature and pressure.  This material is also FDA compliant (21 CFR177.1550).

Performance & Application Information:

These products are designed for applications requiring a quick release/non-stick surface.  This material can operate in temperatures from -100°F (-73°C) to   550°F under dynamic conditions (288°C). This product series has the benefits of dimensional stability, durability, excellent tensile strength and extremely low elongation (<1%).  Applications include: heat sealing platen and element covers, lamination release covers, shrink wrapping, blister packing, plastic bag manufacturing, chute liners, commutator insulation, slot liners, cable & conductor wrapping, belting and many more.

### TYPICAL PROPERTIES

|  | 52-3 | 52-5 | 52-6 | 52-10 | 52-14 | 52-19 |
| --- | --- | --- | --- | --- | --- | --- |
| Nominal Thickness (in.) | .003 | .005 | .006 | .010 | .014 | .019 |
| Nominal Weight (lb./yd²) | .27 | .48 | .54 | .94 | 1.25 | Proprietary |
| Tensile (lbs/in. of width) | 56 | 100 | 100 | 200 | 320 | Proprietary |
| Edge Tear Warp (grams) | 380 | 800 | 800 | 1400 | 3700 | >6400 |
| Edge Tear Fill (grams) | 250 | 700 | 700 | 1100 | 3200 | >6400 |
| Tensile Fill (lbs/sq.in) | 32 | 112 | 112 | 160 | 232 | Proprietary |