| CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com / www.cshyde.com. PRODUCT INFORMATION |
| --- |
| 55-SERIES PTFE (Teflon®) coated Fiberglass Fabric |  |  |  |  |  |  |
| PRODUCT DESCRIPTION |  |  |  |  |  |  |
| The Conductive Grade fabric series is a multi-purpose material that has a slick, non-stick surface. This material is constructed of a carbon filled PTFE (Teflon®) coated woven fiberglass substrate. The 55 Series exhibits exceptional release properties and high resistance to heat, chemicals and moisture. PTFE fluorocarbon resin is one of the most chemically inert materials available. It is also highly resistant to wear, tear, cut through and breakage, even under conditions of extreme temperature and pressure. APPLICATION INFORMATION These products are designed for applications requiring a quick release/non-stick surface and/or high operating temperatures (-70ºF to 500ºF). Applications include: heat sealing platen and element covers, lamination release covers, shrink wrapping, blister packing, plastic bag manufacturing, chute liners, commutator insulation, slot liners, cable & conductor wrapping, belting and many more. |  |  |  |  |  |  |
| PHYSICAL PROPERTIES |  |  |  |  |  |  |
|  | 55-3 | 55-5 | 55-6 | 55-10 | 55-13 |  |
| Nominal Thickness (in.) | .003 | .005 | .006 | .010 | .010 |  |
| Nominal Weight (lb./yd²) | 4.4 | 7.5 | 8.6 | 15.5 | 20.5 |  |
| Breaking Strength Warp (lbs./in.) | 70 | 120 | 120 | 300 | 225 |  |
| Breaking Strength Fill (lbs./in.) | 50 | 100 | 100 | 225 | 175 |  |
| Trapezoidal Tear Warp (lbs.) | 2.0 | 3.0 | 3.0 | 7.0 | 8.0 |  |
| Trapezoidal Tear Fill (lbs.) | 1.5 | 3.0 | 3.0 | 6.0 | 6.0 |  |
| Surface Resistivity (ohms/sq) | 1x106 max | 1x106 max | 1x106 max | 1x106 max | 1x106 max |  |