# CS Hyde Company                               PRODUCT INFORMATION

FAX: 800-441-8063

Silicone Self Fusing Tape,

78-Series

# 1351 North Milwaukee Avenue

## Lake Villa, IL  60046

### TYPICAL PROPERTIES

| Property | Test Method | Performance |
| --- | --- | --- |
| Operating Temperature Range | Continuous | -130˚F to +500˚F |
|  | Intermittent | -145˚F to +500˚F |
| Dielectric Strength, | ASTM D-149 | 0.010” x -0.030” 400 VPM |
| Minimum |  | 0.040” 300VPM |
| Short TIME |  | 0.050” 275 VPM |
| (1/4; Electrodes) |  | 0.070” – 0.080: 200 VPM |
| Dielectric Constant, 1 KHZ |  | 2.95 |
| Dissipation Factor, 1 KHZ |  | <.0004 |
| Volume Resistivity | ASTM D257 | 1 x 10 OHM/CM |
| Cold Brittle Point, MAX | ASTM D-2137 | -65˚C |
| Water Absorption | FED, STD. 601, Method 6251 | 3% Max. by Weight |
| Tensile Strength | ASTM D-412 | 700 PSI Minimum |
| Ultimate Elongation | ASTM D-412 | 300% Minimum |
| Aging Property | ASTM D-412 |  |
| Retention (100 Hrs @ 500˚F) |  |  |
| TENSILE |  | 75% |
| ELONGATION |  | 50% |
| Tear Resistance | ASTM D-624 | 85 PSI |
| Durometer Hardness |  | 50 (+/- 5) Shore Durometer |
|  |  | (Room Cured 24 Hours) |
| Tolerances |  |  |
| THICKNESS |  | +/- .002” |
| WIDTH |  | +/-. 0625” |

Note:   The above values are typical properties and are provided for information only.  They should not be used to set specification requirements.  It is up to the end user to determine whether the material is suitable for the intended application.

# CS Hyde Company                               PRODUCT INFORMATION

800-461-4161 FAX: 800-441-8063		          	Continued

1351 North Milwaukee Avenue

Silicone Self Fusing Tape,

78-Series

## Lake Villa, IL  60046

Product Description:

# Silicone Rubber Self-Fusing Tape is a high performance, extruded wrapping tape. No adhesive is required. SSF Tape is self-adhering, self-fusing and permanent.  It fuses in minutes and cures in 24 hours at room temperature.  Faster curing and a harder finish are accomplished by applying heat after wrapping.  Temperature range is -60°C to 250°C for continuous use; -65C to +260C for intermittent use.

Common Applications:

Automatic wrapping, electrical insulation, moisture protection, high or low temperature applications, SSF is thermally conductive which allows generated heat to dissipate rapidly.  Used in Military, aerospace, industrial motor and marine applications including utility cable terminations and splices, bus bar insulation, motor coil terminal connections, and fuel line and hose repair.  SSF can even be applied UNDERWATER!   Silicone Self-Fusing Tape is the perfect alternative to adhesive electrical tape, duct tape, and heat shrink tape for many applications.  It withstands UV Rays, acids, weather, water and Ozone.