# CS Hyde Company

    - FAX: 800-441-8063

# 1351 N. Milwaukee Ave.

# Lake Villa, IL  60046

## PRODUCT INFORMATION

VT-Series

Colored Vinyl Tape

W/ Rubber Adhesive

Product Description:

# The VT Series is a general purpose, colored SPVC film tape.  It has a clear and colored, stabilized, plasticized, soft polyvinylchloride film backing and a non-corrosive natural rubber adhesive.

Performance & Application Information:

Our VT Series is resistant to moisture and humidity, and has a strong adhesive system as well as a flexible backing.  This tape can be used for floor, lane and aisle marking, color-coding and identification.  It’s also used to wrap and insulate air ducts and underground pipes.  The VT Series can also be used where there is a need for tape to be moisture and humidity resistant.

The VT Series also meets OSHA Color Coding Requirements: Brown-oil; Green-water; Gray-steam; Light Blue-air; Orange-electrical; Red-fire/flammable; Purple-acids/radiation; Yellow-gases; Black and White-miscellaneous.  It also meets the following specifications: A-A-1689 B

### TYPICAL PROPERTIES

|  | Value | ASTM Test Method |
| --- | --- | --- |
| ##### Total thickness | 5.5 mils. | ### D 3759/ D 3715M |
| Tensile Strength (lb./in.) | 18 | D 3330/ D 3330M |
| Adhesion, oz./in. | 117 | D 3652/ D 3652M |
| Elongation % | 150 | D 3759/ D 3715M |
| Operating Temp | 20ºF to 176ºF |  |

FOR MORE INFORMATION CALL 800-461-4161